## Slide 1: Training data
Oxygen vacancy formation energies are calculated using a cubic undistorted A2B2O5 9- atom supercell:
ABO3 perovskite unit cell
: the ground state energy of the defect cell
: the ground state energy of the unit sell
: chemical potential of oxygen (correction is made to the DFT total energy of its ground state)
2 cubic perovskite unit cells with an oxygen removed
5329 compositions
From: A. A. Emery and C. Wolverton, ‘High-throughput DFT calculations of formation energy, stability and oxygen vacancy formation energy of ABO3 perovskites’, Scientific Data, 4:170153, 2017.
The obtained (9 atoms supercell) is comparable with the based on 79-atoms supercell (A. M. Deml et al., Energy Environ. Sci. 7:1996-2004, 2014)
(remove 1 O-atom)

## Slide 2: Validation and test data
 | /eV | Reference
La0.75Sr0.25FeO3 | 3.412 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5FeO3 | 3.344 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.8Ca0.2FeO3 | 3.515 | C. Berger et al., J. of Solid State Chemistry 259:57-66, 2016 (take average value of different Vo sites)
Pr0.8Ca0.2FeO3 | 3.53 | C. Berger et al., J. of Solid State Chemistry 259:57-66, 2016 (take average value of different Vo sites)
Ba0.5Sr0.5FeO3 | 2.22 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
La0.75Sr0.25CoO3 | 2.29776 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5CoO3 | 2.1904 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
Ba0.5Sr0.5CoO3 | 1.21 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
La0.5Sr0.5Co0.5Fe0.5O3 | 2.74504 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.75Sr0.25Co0.5Fe0.5O3 | 2.81664 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5Co0.8Fe0.2O3 | 2.735 | Y. A. Mastrikov et al., Phys. Chem. Chem. Phys., 15:911, 2013
Ba0.5Sr0.5Co0.5Fe0.5O3 | 1.63 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011 (take average value of different Vo sites)
Ba0.5Sr0.5Co0.75Fe0.25O3 | 1.35 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
Ba0.5Sr0.5Co0.25Fe0.75O3 | 1.87 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011 (take average value of different Vo sites)
SrCo0.8Fe0.2O3 | 1.59 | Y. A. Mastrikov et al., Phys. Chem. Chem. Phys., 15:911, 2013
 |  | Reference
La0.75Sr0.25FeO3 | 3.412 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5FeO3 | 3.344 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.8Ca0.2FeO3 | 3.515 | C. Berger et al., J. of Solid State Chemistry 259:57-66, 2016 (take average value of different Vo sites)
Pr0.8Ca0.2FeO3 | 3.53 | C. Berger et al., J. of Solid State Chemistry 259:57-66, 2016 (take average value of different Vo sites)
Ba0.5Sr0.5FeO3 | 2.22 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
La0.75Sr0.25CoO3 | 2.29776 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5CoO3 | 2.1904 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
Ba0.5Sr0.5CoO3 | 1.21 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
La0.5Sr0.5Co0.5Fe0.5O3 | 2.74504 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.75Sr0.25Co0.5Fe0.5O3 | 2.81664 | D. Maiti et al., J. Mater. Chem A 4:5137,2016 (read from diagram)
La0.5Sr0.5Co0.8Fe0.2O3 | 2.735 | Y. A. Mastrikov et al., Phys. Chem. Chem. Phys., 15:911, 2013
Ba0.5Sr0.5Co0.5Fe0.5O3 | 1.63 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011 (take average value of different Vo sites)
Ba0.5Sr0.5Co0.75Fe0.25O3 | 1.35 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011
Ba0.5Sr0.5Co0.25Fe0.75O3 | 1.87 | E. A. Kotomin at al., Solid State Ionics 188:1-5, 2011 (take average value of different Vo sites)
SrCo0.8Fe0.2O3 | 1.59 | Y. A. Mastrikov et al., Phys. Chem. Chem. Phys., 15:911, 2013
Oxygen vacancy formation energy (removing 1 O-atom) calculated by DFT: